## SPECIFICATION FOR APPROVAL

Customer

Product Name     LED LAMP

Part No.     HT-204 SURC

Customer Part No.

Date

| APPROVED SIGNATURES |  |  |  |
| --- | --- | --- | --- |

深圳市宏齐科技有限公司

SHENZHEN HARVATEK TECHNOLOGIES CO.,LTD

| APPROVE | CHECK | DRAW |
| --- | --- | --- |

HT-204 SURC

FEATURES：

- InGaN Red Color

- 3.0mmφ, round top type lamp

- Size：3.0×5.2mm

- Len Color：Water Clear

- High luminous intensity, high reliability and long life

- With ROHS Compliant

APPLICATIONS：

- For display usage.

ABSOLUTE MAXIMUM RATINGS (at TA=25℃)：

| Parameter | Symbol | Min. | Max. | Unit |
| --- | --- | --- | --- | --- |
| Forward Current | IF |  | 30 | mA |
| ###### Pulse Forward Current | IFP* |  | 100 | mA |
| Reverse Voltage | VR |  | 5 | ### V |
| Operating Temperature | Topr. | -25 | +85 | ℃ |
| Storage Temperature | Tstg. | -40 | +100 | ℃ |
| Power Dissipation | PD |  | 120 | mW |

*Pulse width:Max.0.1ms, Duty ratio: Max 1/10

Electrical/Optical Characteristics (at TA=25℃)：

| Parameter | Condition | Unit | Min. | Typ. | Max. |
| --- | --- | --- | --- | --- | --- |
| Forward Voltage VF | IF=20mA | V | 3.0 | 3.4 |  |
| Reverse Current IR | VR=5V | μA |  |  | 50 |
| Dominant WavelengthλD | IF=20mA | nm |  | 465 |  |
| Spectrum width of half value△λ | IF=20mA | nm |  | 30 |  |
| Luminous Intensity IV | IF=20mA | mcd | 3000 | 4000 |  |
| Viewing Angle 2θ1/2 |  | (°) |  | 30 |  |

Parameter Classification

λD(nm)Bin Selection

| ### Blue Color |  |  |  |  |
| --- | --- | --- | --- | --- |
| λD(nm) | Code | λD(nm) | Code |  |
| 451-454 | A | 454-457 | B |  |
| 457-460 | C | 460-463 | D |  |
| 463-466 | E | 466-469 | F |  |
| 469-472 | G | 472-475 | H |  |
| 475-478 | I | 478-481 | J |  |
| No Bin |  |  |  | XX |

IV(mcd) Bin Selection

| ### XX |  |  |  |  |
| --- | --- | --- | --- | --- |
| IV（mcd） | Code | IV（mcd） | Code |  |
| 1000-2000 | A | 3000-4000 | B |  |
| 2000-3000 | C | 4000-5000 | D |  |
| 5000-6000 | E | 6000-7000 | F |  |
| No Bin |  |  |  | XX |

VF(V)Bin Selection

| ### XX |  |  |  |  |
| --- | --- | --- | --- | --- |
| VF（V） | Code | VF（V） | Code |  |
| 2.8-3.0 | A | 3.0-3.2 | B |  |
| 3.2-3.4 | C | 3.4-3.6 | D |  |
| 3.6-3.8 | E | 3.8-4.0 | F |  |
| No Bin |  |  |  | XX |

Package Dimensions：

- All dimensions are millimeters.

- Tolerance is 0.25mm unless otherwise noted.

##### CHARACTERISTIC CURVES：

##### RELIABILITY TEST ITEM AND CONDITION：

| No | Item | ### Test Condition | Sample Number | ### Criteria for Judging | ### Ac/Re |
| --- | --- | --- | --- | --- | --- |
| 1 | Solderability | T=235±5℃ T=5sec. | 15 | ### Good wetting | ### 0/1 |
| 2 | Soldering heat | T=260±5℃ T=10sec. | 15 | #### IV≥LSL* VF≤USL* IR≤USL | 0/1 |
| 3 | Rapid change of temperature followed by： damp heat，cyclic | L:-40℃ 10min （2~3）min H:+100℃ 10min 5cycle T=（25~55）℃ RH：（90~95）% 2cycle 48h recovery time 2h | 11 | #### IV≥LSL VF≤USL IR≤USL | 0/1 |
| 4 | Damp heat，cyclic | T=(25~55)℃ RH=（90~95）% 6 cycle 144h recovery time 2h | 11 | #### IV≥0.7LSL VF≤1.1USL IR≤2USL | 0/1 |
| 5 | Electrical endurance | IF=30mA T=1000h | 22 | #### IV≥0.7LSL VF≤1.1USL IR≤2USL | 0/1 |
| 6 | Storage at high temperature | Tstg=100±2℃ t=1000h | 15 | #### IV≥LSL VF≤USL IR≤USL | 0/1 |
| 7 | Terminal strength | Tensile: W=5N t= 30s Bending: W=2.5N 2times | 15 | No damage | 0/1 |

*U.S.L.: Upper Standard Level

* L.S.L.: Lower Standard Level

PACKAGING：

- Quantity：500 pcs/bag Or 2,000pcs/box

- The package box dimension：

##### APPLICATION NOTES：

- Static Electricity：

Products are sensitive to static electricity and a high standard of care must be taken when handling products. Particularly if an over-voltage which exceeds the Absolute Maximum Rating of Products is applied, the overflow in energy may cause damage to, or possibly result in destruction of the products. To touch the lead directly must be avoided. Customer shall take absolutely secure countermeasures against static electricity and surge when handling products.

Proper grounding of products(via 1 MΩ),use of conductive mat, semiconductive working uniform and shoes, grove and semiconductive containers are considered to be effective as countermeasures against static electricity and surge. The soldering iron point shall be properly grounded.

2)Pb-free Soldering：

Please avoid any stress to LED lamp during soldering.

Recommended soldering conditions are follows：

| ARTICLE | SOLDERING TEMPERATURE | SOLDERING TIME | DISTANCE FROM SOLDERING JOINT TO CASE |
| --- | --- | --- | --- |
| ### SOLDERING BATH | ≤260℃ | ≤4sec. | >2mm |
| SOLDERING IRON | ≤300℃ | ≤3sec. | >4mm |

3) ASSEMBLY ON PCB：

Pin hole pitch on PCB must match lead pin pitch so as not to cause any stress on lead wires.

4) FORMING：

- Any forming on lead pin must be done before soldering, not during or after soldering.

- While forming, please use a tie bar cut or equivalent to hold or bend the pin. Avoid applying any stress to resin for preventing the epoxy fracture and break on bonding wire.

- Avoid bending the lead pin at the same point twice or more.

- CLEANING：

- Alcohol is a recommended method for cleaning.

- Any cleaning method can only be taken under normal temperature in one minute or less.